[image: image1]               TECHNICAL INFORMATION
PLAST CMX
                                                       Code: AM1230

Plastisol ink without phtalate with basic colours for the preparation of  Pantone shades.Suitable to print on t-shirt, sweater, etc. 
GENERAL CHARACTERISTICS

· phtalate free

· bright colours
· high washing resistance at 60° C.
PREPARATION

PLAST CMX can be used with automatic or manual machines.
The use of flash cure units  between the 2 screens simplifies the printing process.

PRINTING
To obtain best result use a screen with 34-90 th/cm both for automatic and manual machines
POLIMERIZATION
Using flash-dryers the printing process will be easier. To obtain washing resistance put in the oven at 160°C for 2-3 minutes. 
THINNER
PLAST ADDENSANTE 740 to increase viscosity (add 0,3% max 4 hours before the use) 

PLAST ADDITIVO UP to obtain puff effect  (add max 20%)
PLAST ADDITIVO 66 to reduce viscosity, to increase brightness (add 5%)

PLAST ADDITIVO 378 to improve printability.
PLAST ADDITIVO 24 to reduce viscosity and improve the printability (add max 1-2% max)

CLEANING
Wash tools with Easicol 842 on press cleaner and Easisolv 701.
CONFECTION
5 – 20 KG.

NOTE

Since it is phtalate free avoid to mix with other plastisol with phtalate.
Before to use it we suggest to make some preliminary test to evacuate if the products fulfill your requirements.
AVAILABLE COLOURS

Giallo light 20, Giallo 22, Arancio 30, Scarlatto 39, Rosso 40, Fuxia 44, Viola 50, Azzurro 51, Blu 56, Blu navy 58, Verde 60, Nero 80,Bianco 80,Trasparente 01.

Amex srl  gives the a/m suggestions as guidelines for the customer and assumes no liability direct or indirect for any improper use.

 It is the  user’s responsibility to determine the suitability of the product to the intended use according to his working conditions.

[image: image3.jpg]


Viale Dello Sport 12 - 22070 Appiano Gentile (CO) Tel. 031 931923
PAGE  
2

[image: image2.jpg]NRAMEXSRL



