[image: image1]                                                                                      TECHNICAL INFORMATION
VINILPLAST OP
                                                                Codice: AM1101
Vinylic screen printing ink with matt finish, suitable for the printing on  adhesive PVC, rigid and soft PVC, polycarbonate, ABS, methacrylate, polistirolo. acrilyc resins.
It is suitable for printing on materials intended to severe use, for instance: foot wears, boots, gloves, etc.
GENERAL CHARACTERISTICS

· F&T (Food and Toys) , lead and heavy metals free, comply to EN71/III
· High covering and printability
· Good external solidity
· It can be over printed.
PREPARATION

Stir the ink before to use. To increase
Add to the ink you need 10-15% of thinner and mix thoroughly.
PRINTING

To obtain best results use screens 150 threads/cm both for manual printing and automatic. Usually 100-120 th/cm.
POLIMERIZATION

By solvent evaporation at room temperature, it can be accelerated with the use of forcerd air oven, according to the hot resistance ofthe material. In this case polimerization takes 20 seconds at 40-50°C.
THINNER

DILUENTE 101 R fast thinner

DILUENTE 102 M medium thinner

DILUENTE 103 L slow thinner

RITARDANTE 104 to slow drying on the screen.

DILUENTE 105 AGGRESSIVO

SOLVENTE LAVAGGIO 109
CLEANING

Wash tools with solvents.
PACKING

1 -5 KG.

NOTE

Before to use the ink in production, we suggest to make some test in order to evaluate if the product satisfies the requirement.
Amex srl  gives the a/m suggestions as guidelines for the customer and assumes no liability direct or indirect for any improper use.

 It is the  user’s responsibility to determine the suitability of the product to the intended use according to his working conditions.

[image: image3.jpg]


Viale Dello Sport 12 - 22070 Appiano Gentile (CO) Tel. 031 931923
PAGE  
2

[image: image2.jpg]NRAMEXSRL



