PRODUCT DESCRIPTION

Plastisol transparent adhesive for textile transfers and hot stamping foil.

GENERAL FEATURES

- Indicated as adhesive for foil

- Indicated as adhesive for textile transfers

- Ideal as adhesive for flock sheets

- Good elasticity and flexibility

- Phthalate-free

PREPARATION

Ready to use.

Homogenize well before using it.

The possible addition of PLAST PF ADDITIVO 378 or PLAST PF ADDITIVO 86 allows to reduce the viscosity.

APPLICATION

PLAST PF TRASPARENTE TRANSFER PLUS is indicated as transfer adhesive. In such application it has to be printed through maximum 43 th/cm screen.

PLAST PF TRASPARENTE TRANSFER PLUS can also be used as foil adhesive. We recommend to print up to a maximum of 34 Th/cm.

PLAST PF TRASPARENTE TRANSFER PLUS can also be used as adhesive for flock sheets. In this case a high deposit of adhesive is recommended.

We advise to use as photo-emulsion the AMEX SCREEN SOL QT BLU.

| FOR TRANSFERS and FLOCK SHEETS (1 mm) | 170°C for 15/18’’ – COLD PEEL |
| --- | --- |
| FOR FOIL APPLICATION | 160°C FOR 15’’ – COLD PEEL |

DRYING (before transfer)

Curing has to take place at 140°C for 1-2 minutes max.

CLEANING

Wash tools with SOLVENTE 108.

PACKAGE

6 – 20 KG.

SPECIAL INSTRUCTIONS

- Always check curing temperature; only an appropriate curing is able to allow the complete ink fusion and so the achievement of the required final characteristics.

- Plastisol inks do not resist to dry cleaning, bleaching and ironing.

- Before using the ink in production, the customer has to make some tests in order to evaluate if the product satisfy requirements.