PRODUCT DESCRIPTION

Solvent based ink with semi-glossy finishing.

PRINTYLON is indicated for printing on nylon fabrics, Tyvek bags, fake-leather and water- proofed fabrics.

The product is also indicated for the realization of sliding and dry decals

GENERAL FEATURES

- F&T (Food & Toys), lead and heavy metals free, comply to EN71/III

- Excellent opacity and printability

- Good outdoor and sea water resistance

- Quick drying

PREPARATION:

Ready to use.

Homogenize before using and dilute the ink according to printing needs.

It is possible to improve the general fastness with PRINTYLON INDURITORE CONCENTRATO in a percentage from 10% up to 20%.

APPLICATION

In order to achieve the best opacity and brightness we recommend to adjust the out of contact and the squeegees pressure.

PRINTYLON can be print with mesh from 77 th/cm to 120 th/cm.

We advise to use as photo-emulsion Amex SCREEN-SOL 200 VIOLA.

POLIMERIZATION

At room temperature by solvent evaporation for 15-20 min.

Polymerization can be accelerated with the use of hot air oven, according to the resistance of the printed material.

In this case the polymerization is at 40-50°C for 20 seconds.

THINNER

DILUENTE 201 R: fast thinner

DILUENTE 202 M: medium thinner DILUENTE 203 L: slow thinner

DILUENTE 209 HR: high resistance thinner

RITARDANTE 204: to slow drying on the screen.

CLEANING

Wash tools with SOLVENTE 108.

PACKAGE

1 - 5 KG.

RANGE

- AM1104.01 TRANSPARENT

- AM1104.10 WHITE

- AM1104.12 SUPER WHITE

- AM1104.20 LEMON YELLOW

- AM1104.21 MEDIUM YELLOW

- AM1104.30 ORANGE

- AM1104.39 SCARLET RED

- AM1104.40 RED

- AM1104.42 CARMINE RED

- AM1104.44 MAGENTA

- AM1104.50 VIOLET

- AM1104.54 ULTRAMARINE BLUE

- AM1104.57 ROYAL BLUE

- AM1104.58 NAVY BLUE

- AM1104.59 DEEP GREEN

- AM1104.80 EXTRA BLACK

SPECIAL INSTRUCTION

- Before to use the ink in production, we suggest making some tests in order to evaluate if the product meets customer’s needs.

- Always check curing temperature; only an appropriate curing is able to allow the complete ink fusion and so the achievement of the required final characteristics.